## Slide 1
Metal Forming – BSc 2026/27-1
Formability

## Slide 2
Topics
Concept of formability
Formability of materials:
  Bulk forming
  Sheet forming
Measurement techniques

## Slide 3
Formability is a mechanical property of a material.
It is characterised by a deformation limit.
As a mechanical property, it is influenced by the so-called state parameters:
    – the state of stress
    – the strain rate
    – the temperature.

## Slide 4
Concept of formability
The plastic deformation is limited by:
– plastic instability
– crack and fracture
Unstable plastic deformation:
At a certain point in the material, the effect of hardening is abrogated by softening.
The source of softening can be:
    – change of geometry,
    – change of the strain rate
    – change of temperature.

## Slide 5
Plastic instability
The plastic deformation is stable in a cylindrical tensile testing specimen if the force increases with increasing deformation:
Plastic instability occurs when:
Force at this case:
Limit of stability:
⇒
where
Next slide

## Slide 6
Plastic instability
Assuming that:
Limit of stability:
Plastic instability occurs when the critical strain is reached; it leads to local plastic deformation (contraction), then fracture of the sample.
Plastic instability can occur during the forming of car body parts, leading to local sheet thinning.
It is beneficial if the value of n is higher.
⇒
⇒

## Slide 7
The limit of deformation. The formability of the material decreases during the forming process. If the strain reaches a critical value (- strain at fracture), fracture occurs.
The limit of the deformation depends on the local temperature, strain rate and stress state. The stress state can be characterised by two quantities:
– Lode parameter ()
– Mayer’s stress state (k)
Plastic strain to fracture

## Slide 8
Mayer’s stress state k
Plastic strain at fracture
+
-
µσ= -1
µσ= 0
Forming limit diagram for bulk techniques

## Slide 9
The occurrence of a fracture can be analyzed by the forming limit diagrams (FLD):
The forming limit diagram of bulk forming processes can be determined by conducting experiments causing different stress states (tensile, upsetting, torsion, bending etc. tests).
The increasing temperature shifts the curves upwards.
The increasing strain rate shifts the curves downwards.
Formability diagram

## Slide 10
Bogatov fracture theory
⇒ fracture
Lode parameter ()
Mayer’s stress state (k)
For continuous forming
For multistep forming
For calculations a fracture theory is needed – Bogatov theory

## Slide 11
The formability for sheet metal forming techniques is characterized by the forming limit diagram (FLD) below.
0
Safe zone
Fracture can be expected
–
+
+
Forming limit diagram (FLD)
Major strain
Minor strain

## Slide 12
Determination of the FLD using Nakazima test
Forming limit diagram (FLD)

## Slide 13
Important quantities of sheet formability from tensile test: – Lankford coefficient (R) – hardening exponent (n).
The R-value characterises the normal anisotropy (perpendicular to the sheet’s plane) of the sheet.
bo
Cross section of the tensile test specimen
so
bo and so are the original, b and s the deformed dimensions. The a is the angle describing the specimen’s orientation relative to the rolling direction of the sheet (see next slide).
R and n values
s
b

## Slide 14
R and n values
Normal
direction
Rolling
direction
Transverse
direction
The a angle
Sheets are always not isotrop!

## Slide 15
The Lankford coefficient is the weighted average of the Ra values measured in the directions 0°, 45° and 90° :
From the Ra values the planar anisotropy of the sheet also can be calculated:
(normal anisotropy)
(planar anisotropy)
R and n values

## Slide 16
The hardening exponent is the exponent of the flow curve which is also direction dependent:
The weighted average of the n values measured in the directions 0, 45 and 90° :
From the na values the planar anisotropy of the hardening can also be calculated:
R and n values

## Slide 17
Example: Stress and strain state during deep drawing
in the flange
in the cylinder
Connection of R and n values to deep drawing
Wish: High normal anisotropy with low planar one

## Slide 18
Lankford coefficient
Hardening exponent
R and n values
DD – good for deep drawing
St – good for stretch forming
DD
St
St
DD
Not good for forming
Only for simple shapes
Lillet diagram
Connection of R and n values to sheet forming technologies

## Slide 19
Jel | C N/mm² | n | R |  |  | 
Carbon steel 0º | 554,7 | 0,1714 | 1,817 | 552,8 | 0,164 | 1,59
Carbon steel 45º | 584 | 0,1619 | 1,067 |  |  | 
Carbon steel 90º | 488,6 | 0,1454 | 2,41 |  |  | 
AlMg3 0º | 461.6 | 0.2914 | 0.613 | 405.4 | 0.2936 | 0.9675
AlMg3 45º | 362.75 | 0.2647 | 1.05 |  |  | 
AlMg3 90º | 434.4 | 0.2937 | 1.157 |  |  | 
R and n values for some materials

## Slide 20
Quantity: displacement of the punch from the contact till the crack of the specimen (mm)
specimen 70x70 mm
Technological tests - Erichsen test
blank holder
punch
die
sphe
sphere

## Slide 21
Starting from Do = 58 mm blank diameter, by 2 mm steps till fracture (up to max. 74 mm).
3 types of punch (flat, rounded, sphere)
Quantity:
Technological tests – deep drawing of a cup
blank
blank holder
die
Cup drawing
33 mm

## Slide 22
Quantity: bending angle till cracking
180 degrees
crack
Technological tests – bending

## Slide 23
Thank you for your attention !